Etching and Deposition Homework –

- (50 pts) Plasma etching of poly Silicon is done at 10 Torr in a gas mixture of 95 mole % CF4 and 5 mole % O2 using an Rf plasma with an electric field strength of 20 V/m operating at 200C.  In the plasma only 1% of the oxygen is converted to free radicals, O*, according the reaction:

O2(g)  2O*

The oxygen free radicals are the attacking agent responsible for the removal of the poly silicon layer according to the reaction:

poly Si(s) + O(g)  SiO(g).

The reaction is first order in oxygen free radicals with a rate constant of 0.9 cm/sec at these conditions.

- What is the average temperature of the electrons in the plasma?

- Do the electrons have sufficient energy to ionize the oxygen free radicals formed?

- Determine the time needed in the plasma etch process to remove 100 nm thick layer of poly silicon assuming that the surface reaction is the rate-determining step.

DATA: mass of the electron = 9.1x10-31 kg, charge of the electron = 1.6x10-19 Coulombs, oxygen atom momentum cross section, m(Vel) is inversely proportional to the electron velocity, Vel , i.e. m(Vel) = {1000 nm2 [m/s]}/Vel, MW Silicon=28 gm/mole, density of poly silicon= 2.33 gm/cm3.

- (50 pts) The Chemical Vapor Deposition of high-quality SiO2 was achieved by reacting Silane, SiH4, and oxygen, O2, in a CVD reactor

SiH4 (g) + O2 (g)  SiO2 (s) + H2(g)

On single wafers chemical vapor depositions were carried out at pressures ranging from 2 to 12 Torr and temperatures between 20 and 300C.  At 250C and 3 Torr total pressure, the data suggest that for molar ratio O2: SiH4 = 11:1 the rate is pseudo first order in Silane concentration.

Rate of SiO2 deposition= koexp(-EA/RT) CSiH4

ko= 1000 m/s, EA= 10*kcal/mole

For these operating conditions, predict the behavior of this reaction in a CVD reactor filled with 100 Silicon wafers.  The wafers are 0.2 mm thick and 30 cm in diameter stacked vertically with a gap of 3 mm.  The length and diameter of the reactor is 10% larger than length and diameter of the wafer stack, respectively.  The total flow rate of all feed gasses is 0.03 mole/min.  For this CVD reactor:

- Determine the conversion of Silane leaving the CVD reactor.

- If the wafers are left in the CVD reactor for 10 min, what is the thickness of the SiO2 deposit on the outside rim of the first (n=1) wafer?

- If the wafers are left in the CVD reactor for 10 min, what is the thickness of the SiO2 deposit on the outside rim of the last (n=100) wafer?

- If the wafers are left in the CVD reactor for 10 min, what is the thickness of the SiO2 deposit at the center of the first (n=1) wafer?

- If the wafers are left in the CVD reactor for 10 min, what is the thickness of the SiO2 deposit at the center of the last (n=100) wafer?

DATA:  MW SiO2 = 60 gm/mole, Density SiO2 = 2.67 gm/cm3, MW SiH4= 32 gm/mole, Molecular diameter, dA= 0.3 nm, Silane Diffusion Coefficient is given by: